Fracture Properties of Wood Surrogates with Adhesives

Date: April 28, 2006

Group: B4

Section: 102

Kevin Clark, Amit Khasgiwala, Jason Phan, Yang Zhang

Background

Glue is current medical practice in gluing cartilages together. Currently, biological adhesives (commonly composed of fibrin, albumin or gelatin) are used in orthopedic operations and fixations are often used to repair defects in cartilages of traumatic origins. In such instances, fractured fragments may be glued back into its original configuration. However, the success of such procedures depends on the adhesive strength of the glue since the fracture energy of the glued-together cartilage is dependent on the ultimate tensile strength of the glue used. In theory, the ultimate tensile strength of a uniform beam is positively correlated with fracture energy, but if the beam is not uniform in composition, its fracture energy is dependent on the ultimate tensile strength of its weakest point. A three-point bending test can be used to accurately measure fracture energy of a sample because it produces pure-bending in the material, in which the primary force acting on the beam is normal to the cross-sectional area of the beam.

In Experiment 4 – “Fracture Properties of Chicken Bones”, five samples composed of one, two, and three pieces of Popsicle sticks with cross-sectional area of 2.00×10-5 m2 were fractured using three-point bending at a loading rate of 5mm/min. (See Appendix, Table 3). The ultimate tensile strength for one piece of Popsicle stick was found to be 3.64MPa ± 0.27MPa (Mean ± SD). All samples fractured at the point where the load was applied. There was also a significant linear relationship between fracture energy and cross sectional area (p=1.9*10-8, Appendix, Figure 2). However, for five samples of chicken bones, there was no significant linear relationship between fracture energy and cross sectional area (p = 0.97, Appendix, Figure 3). In addition, some samples did not fracture at the exact point where the load was applied. A reason to explain these discrepancies is that the bone is not uniform in its composition, and therefore the ultimate tensile strength is different at different points along the bone. Thus, a bone always fractures at its weakest point, or the point where its ultimate tensile strength is the smallest, regardless of its cross-sectional area. This suggests that the fracture energy of bones depends on its lowest ultimate tensile strength. To expand on that previous experiment, this experiment plans to use glue with different ultimate tensile strengths to connect wood surrogates, and observe how that affects the fracture energy of the surrogates.

Aim and Hypotheses:

The aim of this experiment is to compare fracture energies needed to break wood surrogates with and without glues of different adhesive strength, which is the measure of its ultimate tensile strength. The first hypothesis is that glue with a low adhesive strength will yield a lower fracture energy than the surrogate without glue. This is because a lower ultimate tensile strength will result in a decrease in the minimum ultimate tensile strength of the surrogate. The second hypothesis is that glue with a high adhesive strength will not require a higher fracture energy than the surrogate without glue. This is because a higher ultimate tensile strength will not result in an increase in the minimum ultimate tensile strength of the surrogate.

EQUIPMENT:

Major Equipment:

- Instron Model 4444 benchtop materials testing machine

- Customized three-point bending jig

- Computer with LabView data acquisition software

The Instron machine will be required to exert a constant rate of loading on the sample being tested. The customized three-point bending jig will be required to setup the optimal three-point bending test for the sample being tested. The computer with LabView software will be required to record the force and displacement of the Instron machine.

Lab Equipment

- Dial Caliper accurate to 0.01mm

- Straight Ruler accurate to 0.5 mm

- Analytical Balance accurate to 0.0001 g

- Stopwatch accurate to 0.01 second

The dial caliper will be required to measure the cross-sectional area of each sample to high precision since each sample is only about 2mm thin. The ruler will be required to measure the length and width of each sample to determine its axis of symmetry. The analytical balance will be required to measure the weight of each sample to high precision in order to determine the amount of glue applied to each sample. The stopwatch will be used to measure the drying time of glue.

Supplies and Newly Purchased Equipments:

- Popsicle Sticks with dimensions 115mm x 9.50mmx 2.10mm

- Titebond III Ultimate Wood Glue

- Titebond MP300 HiPURformer Polyurethane Hot Melt Adhesive

- Franklin International HiPURformer 1361 Applicator Tool

- 24’’ Adjustable Alloy Bar Clamp

- Exacto Knife

The Popsicle sticks will be the samples being tested in this experiment. The wood glue will be required to serve as an adhesive that has a higher ultimate tensile strength than the Popsicle sticks, and the hot melt adhesive will be required to serve as an adhesive that has a lower ultimate tensile strength than the Popsicle sticks. The applicator tool will be required to apply the hot melt adhesive. The bar clamp will be required to hold together the glued-together sample pieces during drying time. The knife will be required to cut the Popsicle sticks cleanly.

Methods:

- Instron Set-up and 3-Point Bending Testing

  - Please refer to Part A of Experiment 4 – “Fracture Properties of Chicken Bones” in Lab Manual for calibration techniques and set up of 3-point bending jig.

  - Set the crosshead speed to 20 mm/min and sampling rate to 15 samples per second. Measure the distance between the bending jig supports. The set-up should be consistent for all trials.

- Fracturing of Wooden Surrogates

  - Measure the cross-sectional area of each of the wood surrogates (should be approximately 9.50mm x 2.10mm). It is suggested to dedicate some extra surrogates for pilot testing with the Instron to gain familiarity with the set-up of the experiment.

  - Place a surrogate on the bending jig with the 9.50mm dimension laid flat. Using the Instron machine, fracture the surrogate at its midpoint. Collect the force and displacement data on a computer.

  - Using the data, determine the failure load and fracture energy for each surrogate.

  - Using the newly purchased Exacto Knife, cut a separate set of wood surrogates at the midpoint of each surrogate. Ensure that the cut is perpendicular to the surrogate with the use of a straight edge (cutting along the clamp of a dial-caliper). Weigh the mass of both segments on an analytical balance.

- Gluing and Re-Fracturing

  - Take one of the newly cut wood pieces and apply an even amount of Titebond HiPURformer Adhesive on the cross-section with the Franklin International HiPURformer 1361 Applicator Tool. After the adhesive has been applied, reattach its counterpart. Use the bar clamp to continually press together the surrogates. The set time is 10 minutes for bond strength to reach 1.38MPa. Longer set time increases the bond strength. Ensure that the set time is consistent for all trials by measuring the drying time with a stopwatch.

  - After 10 minutes or experimenters designated time, record the amount of adhesive applied by weighing the surrogate again, and then subtracts the mass of both parts obtained from previous weighing.

  - Place the surrogate on the bending jig and fracture with the Instron. The point of the Instron should contact the area of prior fracture. Fracture the surrogate as in Part B above. Measure the new location of fracture. Collect the force and displacement data on a computer, then determine the failure load and fracture energy for each surrogate.

  - For the second set of surrogates, apply Titebond III Ultimate Wood Glue in lieu of Titebond HiPURformer Adhesive in steps 1 and 2. The Applicator Tool is not necessary. For the 10 minute set time, use the bar clamp to press the surrogate fragments together tightly. Then repeat step 3.

PROTOCOL:

- Fracture 5 intact wood surrogates with Instron Machine.

- Cut 10 surrogates at their midpoints.

- Apply two separate glues with different bond strengths (Titebond HiPURformer [1.38MPa at 10 min] and Titebond III Ultimate Wood Glue [27.59MPa]) for each set of 5 cut fragments, respectively. One bond strength should be higher, and the other lower than that of the intact surrogate.

- Identify the fracture location for each surrogate by measuring the distance between the fracture point and the mid-point of the surrogate.

- Use one-tailed and two-tailed T-test to determine if each type of glued sample had a higher or lower fracture energy than the intact samples.

ANTICIPATED RESULTS:

Throughout the course of each trial, the Instron will report the force and displacement data required to fracture the sample (Figure 1), which can then be plotted and fitted with a cubic polynomial regression line. The fracture energy can then be computed by integrating the area under the regression line. Because of the differences in adhesive strengths of the glues applied to the surrogates, the results should yield, on average, that the Titebond III Ultimate Wood Glue required the same fracture energy while the Titebond HiPURformer Adhesive required lower fracture energies—all with respect to the control group of intact surrogates.

| Sample | Fracture Energies (J) |  |  |
| --- | --- | --- | --- |
|  | Control | Titebond III Ultimate Wood Glue | Titebond HiPURformer Adhesive |
| 1 | 0.481 | 0.451 | 0.354 |
| 2 | 0.392 | 0.410 | 0.215 |
| 3 | 0.402 | 0.354 | 0.284 |
| 4 | 0.285 | 0.474 | 0.241 |
| 5 | 0.401 | 0.374 | 0.342 |
| Mean | 0.392 | 0.413 | 0.287 |
| Standard Deviation | 0.070 | 0.050 | 0.061 |

| t-Tests: Two-Sample Assuming Unequal Variances |  |  |
| --- | --- | --- |
|  | Titebond III Ultimate Wood Glue | Control |
| Mean | 0.373 | 0.392 |
| t Stat | 0.46 |  |
| P(T≠t) two-tail | 0.30 |  |
|  | Titebond HiPURformer Adhesive | Control |
| Mean | 0.287 | 0.392 |
| t Stat | 2.53 |  |
| P(T<=t) one-tail | 0.035 |  |

Table 1: Anticipated fracture energies (J) for each group of wood surrogates.

Table 2: T-tests were performed to determine differences in fracture energy between different sample groups.

Load vs. Displacement

0

10

20

30

40

50

60

70

80

90

0.02

0.025

0.03

0.035

0.04

0.045

Displacement (meters)

Load (N)

With No Glue

With Titebond

III Ultimate

Wood Glue

With Titebond

HiPURformer

Adhesive

Figure 1: Typical bone fracture output of the three groups. Wood surrogates glued with the higher adhesive strength and the control group require roughly the same fracture load, followed by surrogates without glue and with glue of lower adhesive strength. The failure load (N) is defined as the maximum force applied before the material breaks, and this is located at the maximum point of each plot.

Two sample t-tests were performed to determine whether or not a significant difference existed between surrogates with each type of glue compared to the control group. From Table 2 above, two-sided and one-sided significance tests showed p-values of 0.30 and 0.035 for the Titebond III Ultimate Wood Glue and the Titebond HiPURformer Adhesive, respectively. Because the p-value of 0.30 for the Titebond III Ultimate Wood Glue (higher adhesive strength) was greater than 0.05, there is no significant difference in required fracture energies at 95% significance level. For the Titebond HiPURformer Adhesive, however, the p-value of 0.035 is less than 0.05, which means the fracture energy with adhesive is significantly less than that with no glue at 95% significance level.

Potential Pitfalls & Alternative Methods/Analysis

There are several potential pitfalls that could arise when performing the experiment. The primary pitfall is that for several reasons the glue could tear prematurely. If either glue is not allowed sufficient time to dry or is not clamped together with enough pressure, then the glue will not reach its maximum adhesive strength. Since the Titebond III Ultimate Wood Glue is expected to have equal or larger fracture energy than the intact sample, if the glue tears prematurely then the experiment is inconclusive. In order to account for this, a drying time longer than the recommended 10 minutes could be given to the sample since for this glue, its adhesive strength does not depend on its drying time after 10 minutes. Also, more pressure could be exerted through the clamp by turning the knob further than normal as long as there is no deformation in the sample.

Even though it is not recommended, the Titebond MP300 HiPURformer Polyurethane Hot Melt Adhesive will be clamped to ensure uniform distribution of the glue. However, error arises because with this type of adhesive, the adhesive strength increases as drying time increases. Therefore in order to ensure precision in the results, each trial must be conducted after the same amount of time has elapsed since application of the glue. In order to decrease this uncertainty, the amount of drying time should be measured with a stopwatch, and samples that have a too long or too short drying time should be discarded. This will allow for more reproducible results.

Another potential source of error is the inconsistency in the cross-sectional area. The surrogates must be cut cleanly and at a 90o angle. If the sample is not cut cleanly, the glue will not bond the two pieces together as strongly, which results in a weaker fracture energy than expected and inconsistent with other trials. If the samples are cut at an angle other than 90o, then when the pieces are clamped together with a large amount of pressure, the pieces could potentially slip and the bond strength would be lower and inconsistent with other trials. This can be corrected by using a straight-edge such as a dial-caliper to measure if the cut is perpendicular to the samples, and then discard the samples that are not cut perpendicularly to ensure consistency.

It is also important to make sure that the same amount of glue is applied uniformly to each Popsicle stick. If less glue is applied to one sample than the others, then that sample will have a lower bond strength and lower fracture energy than the other samples. The best way to verify that equal amounts of glue are applied to each sample is to weigh each sample before and after the glue is applied, then test the samples that have about the same change in mass. However this would mean more samples must be cut and glued together if necessary in order to obtain five samples that are consistent in mass with each other. Furthermore, the glue must be applied uniformly so that no weak points develop resulting in premature fracturing. This can be done by spreading the glue with a brush if necessary.

Lastly, with different glues being applied, the surrogates may fracture at different places, and they may not fracture at a 90o angle. This may create a large variability in the fracture energies within each sample group, which lowers the ability of t-tests to detect any significant differences between the groups. To lower this uncertainty, the angle of fracture for each sample should be measured with a protractor, and samples that fracture at an angle different from 90o should discarded. Increase the number of sample tested can also correct this problem, if there is time left in the experiment.

Budget

| Purchased Item | Quantity per Group | Total Quantity (20 groups) | Price per Unit* | Total Price* |
| --- | --- | --- | --- | --- |
| Popsicle Sticks (115mm x 9.50mm) | 35 | 700 | $5 for 500 | $10.00 |
| Adjustable Alloy Bar Clamp (24”) | 5 | 5 | $24.99 | $124.95 |
| Titebond III Ultimate Wood Glue (16oz) | 1 | 3 | $8.99 | $26.97 |
| Titebond MP300 HiPURformer Polyurethane Hot Melt Adhesive (50g) | 1 | 5 | $6.99 | $34.95 |
| Franklin International HiPURformer 1361 Applicator Tool | 1 | 1 | $69.27 | $69.27 |
| Exacto Knife | 2 | 2 | $1.50 for 5 | $1.50 |
| Total Cost |  |  |  | $267.64 |

*prices do not include taxes or shipping and handling

Popsicle Sticks – The wood Popsicle sticks (114.30mm x 9.50mmx 2.10mm) will serve as surrogate material modeling cartilage. Fifteen sticks are required to perform the experiment. An additional twenty sticks are provided to initially become familiar with the experiment and to allow for error or improperly cut surrogates. This item can be purchased from American Woodcrafters Supply Co. (http://www.awsc-online.com)

Bar Clamp – In each experiment, five clamps are needed to clamp the glued surrogates tightly, and they can be reused. It has a large “wing” type knob for good clamping pressure without causing fatigue. This is necessary to ensure a uniform distribution as well as the maximum adhesion strength of the glue. This item can be purchased from www.woodcraft.com, product #811661.

Titebond III Ultimate Wood Glue – This glue is specifically designed for wood and is necessary for gluing wood surrogates back together. This glue is required for this experiment because it has a higher adhesive strength than that of the normal Popsicle sticks. The literature bond strength at room temperature is 27.59MPa. After application the surrogate needs to be clamped for ten minutes. This adhesive is produced by Franklin International and can be purchased at www.amazon.com.

Titebond MP300 Hot Melt Adhesive – This glue is specifically designed for wood and is necessary for gluing wood surrogates back together. This glue is required for this experiment because it has a lower adhesive strength than that of the normal Popsicle sticks. The adhesive is applied using the HiPURformer™ adhesive applicator at a temperature of 250°F. The literature bond strength at room temperature after ten minutes is about 1.38MPa. This adhesive is produced by Franklin International and can be purchased at www.amazon.com.

HiPURformer 1361 Applicator Tool – This item is necessary to apply the HiPURformer adhesives. One applicator is enough for each experiment, and it can be reused. It is produced by Franklin International and can be purchased at www.amazon.com.

Exacto Knife – This item is necessary to smoothly and straightly cut the Popsicle sticks in half. Two knives are budgeted in one experiment to make the cutting process faster. It can be purchased at www.micro-tools.com.

Appendix

The following data were taken from the previous Experiment4-"Fracture Properties of Chicken Bones", in which five samples composed of one, two, and three pieces of Popsicle sticks with cross-sectional area of 2.00×10-5 m2, as well as five chicken leg bones, were fractured using three-point bending at a loading rate of 5mm/min.

|  | Cross Sectional Area (m^2) | Failure Load (N) | Fracture Energy (J) | Ultimate Strength (MPa) | Angle of Fracture (degree) |
| --- | --- | --- | --- | --- | --- |
| Wood (5 samples per set) |  |  |  |  |  |
| 1 piece | 2.00E-05 | 72.85 ± 5.46 | 0.389 ± .07 | 3.64 ± 5.46 | 90.0 |
| 2 pieces | 3.99E-05 | 152.3 ±11.07 | 0.663 ± .06 | 3.82 ±11.07 | 90.0 |
| 3 pieces | 5.99E-05 | 212.14 ±15.32 | 1.009 ±.11 | 3.54 ±15.32 | 90.0 |

Table 3: Geometry and mechanical failure data of the wood pieces taken from a previous lab experiment: “Fracture Properties of Chicken Bones”.

Figure 2: Fracture energies versus cross sectional area of the wood surrogates. The p-value of the slope is p=1.9*10-8, which means there is a significant linear relationship at 95% significance level.

Figure 3: Fracture energy versus the cross sectional area of five bone samples. The p-value of the slope is 0.97, which means there is no significant linear relationship at 95% significance level.